## Slide 1: High Productivity Reduced Emissions Arc Gouging Process NSRP Project Manager: Mark Smitherman NSRP PTR: Vicky Dlugokecki
NSRP Weld Panel Meeting – August 2023

## Slide 2: Project Team
EWI (prime)
  Jason Rausch (PI), Paul Blomquist (Technical/BD Support)
  Katie Hardin (PM), Mark Schimming (VP Govt Business)
NSRP Program Technical Representative (PTR)
  Vicky Dlugokecki – Naval Architect / Marine Engineer
Participant
  Vigor – Ken Johnson
  BSI EHS – Daniel Chute, Rich Hubner
  CSK Mechanical – Charlie Klangos
Approved for Public Release; distribution is unlimited

## Slide 3: Background
At present, shipyards use carbon arc gouging (CAG) for weld and metal removal:
  Requires extensive protection of large areas
  Generates huge quantities of hot slag that may start fires
  Leaves debris that takes time to clean up
    Even after cleanup, operations typically leave residual carbon dust that could foul electronics and other equipment.
  No other personnel can work in adjacent areas!
Approved for Public Release; distribution is unlimited

## Slide 4
It is entirely possible to eliminate 75% of the labor and materials for “protection” that now must be used to prevent damage to adjacent equipment where CAG is performed.
Significant schedule improvement will accrue. Adjacent operations can be scheduled for work due to the quiet and clean nature of the process.
WeldVac is sufficiently quiet that other operations may proceed nearby. WeldVac tests may demonstrate sound levels below OSHA 90 dBA noise limits, sufficiently quiet that hearing protection would not be mandatory from process operation. Hearing protection may in many cases be mandated by other adjacent metalworking operations or company policies.
WeldVac produces very low levels of smoke and fume. The level of fume generated may well be below existing opacity limits, allowing adjacent operations to be performed, with little need for respirators (unless mandated by other operations or company policy).
Cost of cleanup will be reduced due to capture of nearly all slag and dust.
Another advantage is that a high-pressure air supply is not needed.
WeldVac Potential
Approved for Public Release; distribution is unlimited

## Slide 5
A new approach to gouging and metal removal
Combines a heat source and a vacuum to:
  Melt the material and vacuum out the pool
  Capture the extracted material by water entrainment
  Provide further filtration of effluent if needed or desired
Currently in “Alpha Prototype” stage of development
  Uses standard GTAW power source – other heat sources can be used
  Uses typical shop vacuum – during gouging that’s ALL you hear!
Demonstrated on carbon, stainless steel, and aluminum
  Should work on any conductive material
What is WeldVac?
Approved for Public Release; distribution is unlimited

## Slide 6
Charles Klangos, WeldVac Inventor
WeldVac - Alpha Prototype
Approved for Public Release; distribution is unlimited

## Slide 7
Key: A-Heat Source, B1-Vacuum Nozzle, B2-Vacuum,
C-Capture Chamber
B1
B2
A
C
WeldVac Alpha Prototype
Approved for Public Release; distribution is unlimited

## Slide 8: Alpha Prototype in Operation
Video shot using Visible Welding V2016-Z WeldWatch camera system (www.VisibleWelding.com).
Approved for Public Release; distribution is unlimited
This is a video but I removed it to compress this file to send over email

## Slide 9
WeldVac Shop Gouge Tests
Approved for Public Release; distribution is unlimited

## Slide 10: Objectives
Goal - Reduce the cost and time associated with weld and other metal removal tasks, including new construction, overhaul, maintenance, and repair operations.
Verify that WeldVac methods can produce satisfactory metal removal rates for welds and other materials in U.S. Navy and/or ABS steels and consistently meet the OSHA and other environmental regulations.
Approved for Public Release; distribution is unlimited

## Slide 11: Task 2 – Identification of WeldVac Parameter Sets
A WeldVac system will be set up at EWI.
  Vigor will provide welded test coupons for the target application.
  Parameters for removing the welds for the target application in the selected positions will be developed.
    Metal removal rates, heat inputs, and other data to inform a clear business case analysis will be documented.
A CAG system will be set up at EWI.
  CAG procedures provided by Vigor will be used to remove the welds on the target application in the selected positions.
    Metal removal rates, heat inputs, and other data for the business case will be documented.
Trials will be performed to compare the environmental impact of WeldVac process with the CAG process for the target application.
  BSI Group will be at EWI for these trials and will perform the analysis.
  Trials will be performed with each metal removal process.
  Environmental data will be measured:
    Noise in and around the work area.
    Air monitoring including personal breathing zone and area air sampled for calculation of total weld fume and respirable particulates.
Approved for Public Release; distribution is unlimited
I think we should delete the last 2 major bullets since the comparison won’t happen

## Slide 12: Video from Setup/Training at EWI
Approved for Public Release; distribution is unlimited
This is a video but I removed it to compress this file to send over email

## Slide 13: Progress
Successful gouge lengths of 6” to 21”
  220 AMP / 30-35 IPM
Approved for Public Release; distribution is unlimited

## Slide 14: Technical Difficulties to Work Through
Slag buildup in aluminum hose
  Consistently clogging the nozzle to result in stopping weld to clean out
Aluminum nozzle
  Design – working with inventor to determine best design for this nozzle
  Steps inside barrel – potentially contributing to slag buildup
    EWI having a one-piece barrel made with the same diameter as the vacuum hose
Approved for Public Release; distribution is unlimited

## Slide 15: Task 3 – Shipyard Demonstration
The WeldVac system will be shipped to Vigor and set up in the shipyard’s Weld School.
  Trials will be performed by shipyard personnel using the parameters developed in Task 2 for the target application.
  Demonstration of the WeldVac system will be performed for project participants.
  A description of the trials, metal removal rates, and other relevant data will be documented.
  Feedback from shipyard personnel who attend the demonstrations will be documented.
Approved for Public Release; distribution is unlimited

## Slide 16: Task 4 – Technology Transfer and Reporting
Brief NSRP Environmental, Health, and Safety Panel
Quarterly reports
Final written report - documents background, technical approach, results and conclusions
Approved for Public Release; distribution is unlimited

## Slide 17: Questions?