## Slide 1: Alternate Blocking Materials
NSRP Panel Project PP 23-018
Final Presentation
12 March 2024

## Slide 2: Rights & Technology Transfer
2
Category B Funding:
Data developed partially with funding from project participants that was not charged to a government contract, and partially with government funding.
Distribution:
Distribution unlimited.

## Slide 3: Outline
DM Consulting Introduction
Introduction to Drydocking
Traditional Methods of Block Construction
Proposed New Materials
Other Research and Examples
Cost Comparison
Implementation
Conclusion

## Slide 4: DM Consulting – Dry Dock Experts
Established 2000
Certified Dock Masters
Training
Consulting
Dry Dock Acquisitions
Dry Dock Modernization
  Block Contact Indicator System
  Dock Master Software Development
  Underwater 3D Scanning
  Syncrolift Shiplifts and Fast Docking System
  IDAC West Floating Dry Dock Control System

## Slide 5: Drydocking
5

## Slide 6: Drydocking
6
Keel Blocks
Support most of a ship’s weight

## Slide 7: Drydocking
Side Blocks
Keep vessel upright

## Slide 8: Drydocking
8
8

## Slide 9: Example of Wood Used (DDG)
9
7.5 ft block height (shaft removal)
5.5 ft base block + 2 ft of soft wood
80 Blocks total (KB + SBs)
Max SB height = 5 ft
~2600 ft³
Softwood lifespan = 2 years
Rubber lifespan = 10 years
9

## Slide 10: Block Construction History
10
10

## Slide 11: New Materials
High Density Polyethylene (HDPE)
  Goal is to replace soft wood caps
Neoprene Pads
  Goal is to replace soft wood caps
Fiber Reinforced Concrete Blocks
  Goal is to replace traditional steel reinforced concrete blocks

## Slide 12: HDPE
12
Similar to wood in strength, construction, & density
Completely waterproof & UV Stabilized
Will not rot
Can be easily repaired without having to be replaced.
Can be constructed from recycled plastic and can be recycled at end of useful life.

## Slide 13: Neoprene Pads
13
Readily available world wide
Will provide better flexibility than wood
Will not rot
When bonded with steel plates top and bottom, should have an expected service life of 20 years.

## Slide 14: Fiber Reinforced Concrete Blocks
14
Quicker to produce blocks
Blocks tend to spall less, lengthening service life
Same or better strength for same value
Typical Concrete block spalling due to steel reinforcement
Fiber concrete mix

## Slide 15: Benefits
15
All materials are expected to have a longer service life (expected approx. 5 times soft wood)
All materials can be recycled at the end of their service life
All materials are expected to have similar or better mechanical properties than current technology
The proposed materials are new to our industry, but they are not new materials

## Slide 16: Other Research Projects
Docking Block Revolution Presentation
  By the Docking Office at JRMC Yokosuka, JP
  Idea was use it for curved blocks without cutting to shape
  Undefined material make up
  Undefined block flexibility effects on other aspects of analysis

## Slide 17: Other Research Projects
Fiber-Reinforced Rubber Blocks Presentation
  By Shibata - a fender manufacturer
  Conforms to hull, fiber adds rigidity
  Undefined material make up
  Undefined block flexibility effects on other aspects of analysis
Fiber-reinforced rubber block section

## Slide 18: Other Research Projects
Engineering and Economic Feasibility of Using Rubber Soft Caps For Drydocking of Naval Vessels
  By LCDR Vincent C. Watson, FL
  Engineering behind use for curved blocks without cutting to shape
  Undefined material make up
  Undefined block flexibility effects on other aspects of analysis

## Slide 19: Other Known Use Cases
Based in Australia
No longer in business under this name.

## Slide 20: Other Known Use Cases
UK Navy
Submarine Facility

## Slide 21: Other Known Use Cases

## Slide 22: Cost Comparisons
22
22
Example Case of Using HDPE or Neoprene instead of soft wood for the soft cap
60 Concrete blocks, topped with hard wood and a soft wood cap
Block length = 3.5’
Block Width = 4’
Soft Cap = 2”
Soft Cap Vol = 210 cu ft
Assume 6 dockings per year
Assume 1 hour for a crew of 3 at $40 / hour labor

## Slide 23: Cost Comparisons
23
23
Description | Wood 2x4x8 Yellow Pine | HDPE 54x48x1/2 Marine Grade | Neoprene Pads
Volume per Piece (cu ft) | 1.5” x 7.5” x 8’ = 0.292 cu ft | 54” x 48” x ½” = 0.75 cu ft | 1 per block
Quantity | 720 | 280 | 60
Unit Cost | $3.35 | $256 | $2,538
Extended Cost (Initial Cost) | $2,412 | $71,680 | $152,280
Labor Cost | $7,200 | $7,200 | $7,200
Install Cost | $9,612 | $78,880 | $159,480
% Replacement per Docking | 100% | 5% | 2%
Annual Maintenance Cost | $57,672 | $23,664 | $19,138
10 Year Cost | $586,332 | $315,520 | $350,856

## Slide 24: Cost Comparison
24
24
Fiber Reinforced blocks will cost approximately the same as traditional blocks.
Expected life span 33% more than traditional reinforced blocks (15 yrs vs. 20 yrs)

## Slide 25: Implementation
25
25
Gulf Copper Shipyards, Port Arthur and Galveston, TX
  Testing HDPE & neoprene caps
  Tug
  Offshore Work Vessel
  USACE Vessel
Mare Island Dry Dock, Vallejo, CA
  Testing fiber reinforce concrete blocks
  Coast Guard Vessel

## Slide 26: Material Testing
HDPE/Neoprene – Offshore Work Vessel

## Slide 27: Material Testing
HDPE/Neoprene – HDPE Block
Notes: HDPE

## Slide 28: Material Testing
HDPE/Neoprene – Neoprene Block
Notes: Neoprene

## Slide 29: Material Testing
29
HDPE/Neoprene – Strength Testing
HDPE Material Testing Results |  | 
Nominal Material Thickness | Yield Strength (Control) | Yield Strength (Post Dockings)
1/2 inch | 870 psi | 1,100 psi
3/4 inch | 780 psi | 1,080 psi
1 inch | 960 psi | 1,120 psi

## Slide 30: Material Testing
30
HDPE/Neoprene – Friction Testing

## Slide 31: Material Testing
31
HDPE/Neoprene – Friction Testing Results
Friction testing of HDPE yielded 50% friction coefficient of wood in some test conditions.
HDPE manufacturer stated a friction coefficient of 0.2 for both a greased and ungreased surfaces.
Neoprene friction testing yielded similar results to wood.

## Slide 32: Material Testing
32
HDPE/Neoprene – Friction Engineering Analysis
Results | 
µ | ϴ [deg]
0.05 | 2.9
0.10 | 5.7
0.15 | 8.5
0.20 | 11.3
0.25 | 14.0
0.30 | 16.7
Seismic Overturning Force
Reference: US Standard Drydocking Calculations from NSTM 997
EAF = 0.2
µ = 0.2

## Slide 33: Material Testing
HDPE/Neoprene – USACE Vessel Blocking Plan

## Slide 34: Material Testing
HDPE used with Rotating Side Block
Block Contact Indicator System seen here
HDPE – Example use
Notes: Neoprene

## Slide 35: Material Testing
35
Fiber Reinforced Concrete Blocks – Example use
Fiber block under a
US Coast Guard Vessel

## Slide 36: Material Testing
36
Fiber Reinforced Concrete Blocks – Testing
Testing completed by independent material testing laboratory:
Testing Engineers, CA

## Slide 37: Material Testing
37
Fiber Reinforced Concrete Blocks – Viability
 | Compressive Strength |  | Splitting Tensile Strength
 | [PSI] |  | [PSI]
Old Navy | 7500 |  | 548
New Fiber | 8970 |  | 902
Old Fiber | 7850 |  | 662

## Slide 38: Project Challenges
38
Lead time of material ordering presented challenges.
Navy drydocking canceled at NBSD after dry dock reorganization. However, Coast Guard and USACE Vessel
vessels were involved.
2 separate government agencies showed interested, but ultimately couldn’t engage with the project within the panel project time frame.
Calculating carbon footprint due to inconsistent measuring techniques.

## Slide 39: Conclusion
39
Neoprene – More testing and research needed
Material is difficult to work with compared to wood. Special tooling/fasteners required.
Cost is much higher than HDPE or wood.
Not recommended as tested.
May require special NAVSEA approval for use on Navy operations.

## Slide 40: Conclusion
40
HDPE – Proceed with restrictions
Good workable substitute for softwood.
Monitor and replace damaged HDPE as normal. Regular testing/inspections recommended.
Potential friction hazard. Recommend limit 25% unscored HDPE per docking. Not recommended for use in earthquake prone areas until additional research completed.
Currently available in sheets, not serviceable for curved side blocks, however industry adoption could change this.
May require special NAVSEA approval for use on Navy operations

## Slide 41: Conclusion
41
Fiber Reinforced Concrete – Ready to implement
Utilized in many structural projects in other industries.
Utilize engineered design for fiber reinforced construction.
Expert help to determine the right fiber/concrete mix.
Test sample to verify compression strength and inspect at regular intervals.
May require special NAVSEA approval for use on Navy operations.

## Slide 42: Recommendations Future Testing
42
HDPE/Neoprene
Yield strength increase post-docking.
Friction analysis.
Hot work environments. So far, no issues.
Extreme cold weather. Untested, not anticipated.

## Slide 43: Additional Information
43
Please see our final paper for more in-depth analysis.
Available on:
DM Consulting Website:
DryDockTraining.com/Alternate-Blocking-Materials.html

## Slide 44: Thank you
Acknowledgements
Gulf Copper Shipyard, TX – Neoprene and HDPE Testing
Mare Island Dry Dock, CA – Fiber Reinforced Blocks Testing
Kirsten Walkup, GD BIW, ME, Sustainment Panel Chair
Kaipo Crowell, Sustainment Panel vice-chair/PTR
Jim House, ATI Project Manager
Mark Smitherman, ATI Deputy Director
ATI Contracts Team
NBSD Graving Dock, CA – Navy Sponsor
Austal USA, CA – ECB Sponsor